## Slide 1
Investigating the Excited State Properties of Photoactive TiO2 Nanoclusters through Non-Adiabatic Molecular Dynamics
Miguel Recio-Poo, Francesc Illas, Stefan T. Bromley, Alexey V. Akimov, Ángel Morales-García
Departament de Ciència de Materials i Química Física
Institut de Química Teòrica i Computacional (IQTCUB)
Universitat de Barcelona
miguelrecio@ub.edu

## Slide 2
OUTLINE
Motivation and previous research
Methodology - Libra/CP2K workflow
First project: role of water and benchmark analysis
Second project: recombination or relaxation in small bare NPs
Conclusions
LIBRA Summer School 2024
2/30
Miguel Recio Poo

## Slide 3
Chemical energy
𝚫G0= 237 kJ/mol
Energy
H2O
Clean energy production but against thermodynamics
Need of external energy -> photocatalytic water splitting
Anatase titania (TiO2) nanoparticles potential solution
BG is too large. Absorbs only a small fraction of solar spectrum.
It is inert enough, and can be functionalized -> DSSC
Water splitting: a simple idea
H2O H2 + ½ O2
TiO2
H2
O2
LIBRA Summer School 2024
3/30
Miguel Recio Poo

## Slide 4
Previous research
Previous studies based on time-domain version of the Kohn-Sham DFT (KS-DFT):
A single-particle treatment inadequate for quantitative characterization of the dynamics in systems as TiO2 nanostructures. More rigorous (linear-response, LR) time-dependent DFT (TD-DFT) framework needed.
LIBRA Summer School 2024
4/30
Miguel Recio Poo

## Slide 5
Previous research
Lack of research concerning the influence of water on photoactive nanostructures when adsorbed in their surfaces
Non-Adiabatic Molecular NA-MD trusted as the suited technique to investigate the dynamics of excited states
LIBRA Summer School 2024
5/30
Miguel Recio Poo

## Slide 6
Methodology - Libra/CP2K workflow
CP2K: step 1, step 2 (excitations)
Libra: step 2 (overlaps), step 3, step 4
LIBRA Summer School 2024
6/30
Miguel Recio Poo

## Slide 7
First project: water effect and benchmark analysis
(TiO2)4
(TiO2)4(H2O)2
(TiO2)8
(TiO2)8(H2O)2
(TiO2)8(H2O)5
Benchmark the used TD-DFT and NA-MD methodologies for their further applications to bigger photoactive nanostructures
Investigate the dependence of static excited state properties and excited state dynamics on the nanocluster size and hydration degree.
(TiO2)4(H2O)4
LIBRA Summer School 2024
7/30
Miguel Recio Poo

## Slide 8
First project: water effect and benchmark analysis
GULP: Classical MD (NanoTiO & FFTiOH IP)
CP2K: AIMD (PBE), xTB
NVT ensemble. Target temperature: 300 K
4 ps run (1 ps equilibration + 3 ps production)
1 fs timestep → 3000 different geometries
LIBRA Summer School 2024
8/30
Miguel Recio Poo

## Slide 9
First project (step I)
The atomic vibrational frequencies of our titania clusters along the 3000 fs runs let us easily compare the performance of either methodology.
Vib. modes at frequencies similar to those observed in titania bulk phase
100 to 200 cm-1 -> Ti-O stretching modes 500-1000 cm-1 -> Ti-O-Ti angle bending
Hydrated (TiO2)8 clusters: characteristic hydroxyl stretching mode around 3700-3900 cm-1 values2
LIBRA Summer School 2024
9/30
Miguel Recio Poo

## Slide 10
First project (step I)
Anharmonic effects in AIMD approach -> lower frequency values but also busier vibrational densities
Power spectra are qualitatively the same -> tested FFs are accurate to act as computationally-efficient counterparts to DFT calculations
LIBRA Summer School 2024
10/30
Miguel Recio Poo

## Slide 11
First project (step II)
S0 to S1 state transition (but we include up to ten TD-DFT excited states)
PBE, PBE0 and B3LYP functionals
MB representation
Time-overlaps between consecutive geometries,
LIBRA Summer School 2024
11/30
Miguel Recio Poo

## Slide 12
First project (step II)
LIBRA Summer School 2024
12/30
Miguel Recio Poo
FT of δEij gives rise to the influence spectra, which shows up the vibrational modes responsible for S0 to S1 transition
(TiO2)8(H2O)0
Bare case: S1S0 transition is driven by the Ti-O-Ti angle bending mode
Hydrated clusters: driven by bending and stretching modes
Hydroxyl related modes not coupled to the S1S0 transition
(TiO2)8(H2O)5

## Slide 13
First project (step II)
LIBRA Summer School 2024
13/30
Miguel Recio Poo
Larger electronic densities located around the Ti-O bonds. Consistent with the spectra.
Excited state of bare shows larger transition dipole moment. Increasing degree of hydration -> excited state becomes more symmetric, leading to smaller TDM

## Slide 14
First project (step III)
LIBRA Summer School 2024
14/30
Miguel Recio Poo
Hammes-Schiffer-Tully (HST) approach for computing NACs:
where stands for the time overlaps computed in the previous step

## Slide 15
First project (step III)
LIBRA Summer School 2024
15/30
Miguel Recio Poo
(TiO2)8(H2O)0
(TiO2)8(H2O)2
(TiO2)8(H2O)5
(TiO2)8(H2O)2 presents lower average NACs than bare case (states more separated in energy)
For largest degree: the states acquire similar spatial distributions
Fully hydroxylated system possess better electronic state mixing and thus larger NACs

## Slide 16
First project (step IV)
LIBRA Summer School 2024
16/30
Miguel Recio Poo
Pre-computed energies () and NACs (are used to construct the vibronic Hamiltonian at every timestep of the trajectory
Trajectory surface hoping (TSH) algorithms: FSSH, mSDM, DISH, IDA
30 initial conditions x 500 realizations = 15000 trajectories per methodology. NA-MD runs are initialized in S1 in all of them. Decay evolution fitted to exponential fitting functions

## Slide 17
Files: 1500-1600
Files: 500-800
Method: FSSH, ntraj: 200
Files: 1500-1800
Files: 2000-3000
(TiO2)4 (H2O)4 AIMD + B3LYP
We can play with which NACs and excitation energies we select and avoid the problematic step causing the sudden population change
✅
First project (step IV-problematics)
LIBRA Summer School 2024
17/30
Miguel Recio Poo

## Slide 18
First project (step IV-problematics)
LIBRA Summer School 2024
18/30
Miguel Recio Poo
(TiO2)4 (H2O)4 AIMD + B3LYP
Method: FSSH, ntraj: 200, files: 1000-4000, steps: 3000
If we include 5 states in our dynamical basis… we have these sudden changes in Ground State population evolution

## Slide 19
(TiO2)4 (H2O)4 AIMD + B3LYP
By increasing the number of excited states in our dynamical basis -avoiding crosses with states that are not included in the basis- we can overcome our problem with the sudden changes in states pop. evolution
Method: FSSH, ntraj: 200, files: 1000-2000, nsteps: 2000
NSTATES = 5
NSTATES = 10
First project (step IV-problematics)
LIBRA Summer School 2024
19/30
Miguel Recio Poo

## Slide 20
First project (step IV)
(TiO2)4
(TiO2)4(H2O)2
FSSH
DISH
MSDM
ID-A
AIMD + PBE
(TiO2)4(H2O)4
In all cases FSSH yields shorter e--h+recombinationtimes
Faster recombination evolution with increasing degree of hydroxylation
LIBRA Summer School 2024
20/30
Miguel Recio Poo

## Slide 21
First project (step IV)
mSDM method involves a complex description leading to the elimination of coherences and thus to larger decay
Hybrid TD-DFT functionals give rise to faster S1-S0 recombination
Good agreement in final results between ffMD and AIMD!!
(TiO2)8(H2O)2 provides longer times – more convenient for photocatalysis
LIBRA Summer School 2024
21/30
Miguel Recio Poo

## Slide 22
Second project: recombination or relaxation?
sub-picosecond excited state lifetime (τ) is attributed to rapid internal conversion returning to the ground state.
LIBRA Summer School 2024
22/30
Miguel Recio Poo

## Slide 23
Second project: Wigner sampling
RUN GEOMETRY OPTIMIZATION WITH CP2K
+ CALCULATION OF VIBRATIONAL FREQUENCIES
RUN wigner.py SCRIPT
(-n 100) (-t 300)
10 GEOMETRIES + VELOCITIES:
RUN STEP1, STEP2 (CAM-B3LYP), STEP3, STEP4
initconds file
COMPUTE AVERAGE VALUES
TiO2_01-VIBRATIONS-1.mol
LIBRA Summer School 2024
23/30
Miguel Recio Poo

## Slide 24
Average timescale: 26.34+-7.94 ps
Average timescale: 915.95+-64.22 ps
Second project
Several orders of magnitude bigger than the experimental times
LIBRA Summer School 2024
24/30
Miguel Recio Poo

## Slide 25
Average timescale: 5.00+-2.08 ps
Average timescale: 33.67+-14.65 ps
Second project
Several orders of magnitude bigger than the experimental times
LIBRA Summer School 2024
25/30
Miguel Recio Poo

## Slide 26
Second project: trajectory aligment
Average timescale: 17.89+-1.09 ps
Average timescale: 41.56+-5.64 ps
LIBRA Summer School 2024
26/30
Miguel Recio Poo

## Slide 27
Second project: Oscillator Strength TiO2
LIBRA Summer School 2024
27/30
Miguel Recio Poo

## Slide 28
Second project: TiO2
✅
LIBRA Summer School 2024
28/30
Miguel Recio Poo

## Slide 29
5. Conclusions
Libra (interchanged with CP2K) provides a complete workflow to analyse excited state dynamics in titania systems.
Influence of water in general reduce recombination times, as NACs increase. Methodology assessment: ffMD is efficient counterpart to AIMD. Hybrid functionals give rise to faster S1-S0 recombination.
Small anhydrous calster undergo fast relaxation among optical levels that has been overlooked in experimental research.
ESPA Tarragona 2024
Conclusions
LIBRA Summer School 2024
29/30
Miguel Recio Poo

## Slide 30
Stefan T. Bromley
Ángel Morales García
Francesc Illas
ACKNOWLEDGMENTS
Alexey V. Akimov
LIBRA Summer School 2024
30/30
Miguel Recio Poo